## Slide 1: Oil and Grease Resistance Test Methods SNP Inc.

## Slide 2
Most common OGR test methods
3M® Kit Test (Tappi T559)
Turpentine Test (Tappi T454)
Permeability Test (ISO 16532-1)

## Slide 3
3M® Kit Test
  Well-known by paper and board manufacturers and suppliers
  Measures the degree of repellency of paper or boards treated with fluorochemical sizing agents
  Used to quantify and compare performance of cellulose substrates used for food contact and other packaging applications
  Easy, cheap, quick and reproducible

## Slide 4
Turpentine Test
  Utilizes silica sand in conjunction with dyed turpentine
    Time taken for dye to penetrate substrate is then determined
  Not always the most suitable method for assessment of cellulose substrates having grease or oil resistance through use of coating or internal treatment

## Slide 5
Permeability Test
  Determines the grease resistance of both creased and uncreased cellulose substrates by determination of time taken for palm kernel oil (a simulated fat material) to penetrate into fibers
  Method is equally applicable to cellulose substrates that have been internally or surface sized with organophobic materials, or plastic coatings

## Slide 6
Comparison of OGR Testing Methods

## Slide 7
3M® Kit Test Solution Compositions

## Slide 8
Surface Tensions of 3M® Kit Test Solutions
Wetting of surfaces by liquid is ruled by
surface tesnion of liquid vs. surface energy of solid
Liquid
 = contact angle
Solid surface
S = surface energy of solid
L = surface tension liquid
Liquid wets completely solid if L < S


## Slide 9
3M® Kit Test
FAIL
PASS
#1
#2
#3
#4
#5
#5
#5
#5
Passed #4, failed at #5. Kit Value =#4.

## Slide 10
Problem with Kit Test Use to Predict OGR Performance in Use
It does not always correlate with in-use performance due to the presence of solvents in test solutions
Coatings providing good oil and grease resistance but poor solvent resistance will fail therefore not accurately predicting in-performance use
Does not account for hydrostatic pressure exerted by packaged goods
In-use performance of non-fluorochemical containing coatings and papers can not be predicted by this test method
Foods do not contain solvent

## Slide 11
Prepare colored turpentine test fluid by adding 5 grams of anhydrous calcium chloride and 1.0 gram of a suitable oil-soluble red dye to 100 grams of turpentine in a capped bottle.
Shake well and let stand for at lease 6 hours, shaking occasionally.
Warm solution to approximately 70 deg F.
Filter solution through a dry filter paper.
Place back in air tight capped bottle.
Preparation of Turpentine Test Solution

## Slide 12
Turpentine Test Procedure
Using a pencil, mark a 72 x 72 inch square on the treated side of the specimen to be tested. The specimen should be free of creases or folds and should be placed a smooth flat surface.
Using a stencil brush apply the turpentine test solution to the specimen.
Start timer and time 60 seconds.
Wipe surface and count # of pinholes present. Test at least 6 specimens and report maximum and minimum of pinholes observed.

## Slide 13
Permeability Test-TAPPI T-507
Pressure block 720g
Oil Indicator
The prepared paper 100mm x 100mm
Saturated blotting paper 75mmx75mm
Clean blotting paper 100mm x 100mm
Aluminum foil 100mm x 100mm
Pressure block 720g

## Slide 14
Hot Mazola Test Procedure
Weigh specimen on balance with accuracy of 0.001g or better.
Set-up and test as if running a Cobb test (TAPPI T-441), except replace water with corn oil.
Place specimen in a 110 degree C oven for 20 minutes.
After 20 minutes, remove from oven and pour off oil.
Remove specimen from Cobb tester.
Place two standard blotter sheets over specimen and remove excess oil by moving a roller having a smooth face 20 cm wide and weighing 10.0 ± 0.5 kg (22 ± 1.1 lb) over its surface.
Reweight the specimen and calculate the amount oil absorbed/unit area of the test specimen.
**Note if staining is observed. If oil penetrates specimen mark as failed.

## Slide 15
Oleic Acid Test Solution Compositions
Test Composition (%w) |  |  | 
Solution # | %Castor Oil | %Oleic Acid | %Octanoic Acid
1 | 100 | 0 | 0
2 | 50 | 50 | 0
3 | 30 | 70 | 0
4 | 0 | 100 | 0
5 | 0 | 80 | 20
6 | 0 | 70 | 30
7 | 0 | 55 | 45
8 | 0 | 35 | 65
9 | 0 | 20 | 80
10 | 0 | 10 | 90
11 | 0 | 0 | 100

## Slide 16
Procedure
Place specimen inside a preheated 60 degree oven on a flat surface with side to be tested facing up.
Without touching dropper to the surface of the paper, place one drop of each test solution onto the surface of the paper. Drop height should be 1-2 cm.
Close the oven and start timer.
After 6 min, remove sample from oven and wipe excess reagent from the surface with an absorbent material.
Evaluate the surface of the sample at each drop placement area and note if penetration, dark staining, or pinholes are observed.
Record highest # reagent that did not cause failure (penetration).
Record highest reagent# for which no visual staining was observed.
Report presence of pinholes as “Yes” or “No”.

## Slide 17
RP-2 OGR Performance Test
Store at 60 C for 24 hrs.
Report stained squares as percent failure.
Red stained RP synthetic oil (Ralston-Purina proprietary)
Ottawa sand (5g, 20-30 mesh)
Treated paper sample
(Creased on diagonals)
Grid printed sheet (10x10cm)

## Slide 18
Pet Food Performance Test
Conditions:
Temp. = 60-70 °C
R.H. = 50-65%
Duration = 16-24 hours
Report results as % stained surface

## Slide 19
Surface tension (dynes/cm)
31-32
Cooking oil (2)
40 - 50
Untreated paper (1)
27-28
Free fatty acids (2)
6
CF3 monolayer (3)
18
-CF2- sequence (PTFE) (3)
Natural fats and oils
Ideal CF2 coverage
Ideal CF3 coverage
Values detected at 20°C
Source: (1) Borch J., J. Adhesion Sci. Technol., 5(7), 523 (1991(; (2) Solvay Solexis internal data (3) Zisman W.A., Contact Angle, Wettability and Adhesion, Advances in Chemistry Series, Vol 43 (1964) and refs. teherein
Surface tension values of liquids and surfaces

## Slide 20
Paper Wetting Mechanisms by Oils/Fats

## Slide 21
Low polarity/Low reactivity
R = C6 to C22
Polarity/Reactive groups
Fats/Oils Chemical Structure

## Slide 22
A) Non-polar, non-reactive oils
- surface energy of treated paper vs. liquid surface tension - solubility effects
- capillary adsorption contribution
B) Reactive, polar oils
- polar interaction with paper constituents
*Both mechanisms need to be considered when formulating a coating
to meet application requirements
Parameters Affecting Oil Adsorption

## Slide 23
Fatty acid composition of natural oils and fats (contained as tryglicerides)
Oils and Fats Composition

## Slide 24
How do different carbon chain lengths in Free Fatty Acids (FFA) affect penetration?
Penetration through the coated substrate is related to the carbon chain length.
The greater the number of lower carbon chain free fatty acids will result in more aggressive penetration of FFA.
Fatty Acids Penetration

## Slide 25
Free Fatty Acids in Packed Materials
Pet Foods
  Generally containing from 10 to 27% crude fat
  Crude fat contains 10 to 30% FFAs by weight
  FFAs in pet-food materials can range from 1 to 9%
Butter
  W/O emulsions
  Triglycerides hydrolysis takes place
Chicken Fat
  May contain up to 10% FFA

## Slide 26: FFA Alternative to Kit Test

## Slide 27
Test fluids increase in aggressiveness as percent of shorter chain FFA increase
Unlike kit solutions, there is little variation in surface tension of fluids over time
Test Solutions: 5 Fatty Acids Mixtures

## Slide 28
Test fluids are more reflective of what will be seen in use.
Test fluids contain no solvents.
Temperature of 60C can be used to accelerate test results.
Test fluids are stable over time.
Benefits of Test Method

## Slide 29
Apply test fluids in same manner as kit solutions.
Keep mixtures in oven at 60°C prior to use.
Place sample with test fluieds in oven at 60°C for 10 minutes.
Remove from oven and observe staining.
Paper is rated with the # of highest mixture that does not stain.
Fatty Acid Test Procedure
Fail
Pass